## Slide 1: Silicon Photonics for high bandwidth communications

## Slide 2: Why silicon photonics ?
Silicon photonics aims at integrating in the silicon microelectronic CMOS technology optical functions initially based on other technologies (InP, InGaAs, LiNbO3, SiO2, …)
Need for integration is driven by:
  Miniaturization: cost&size reduction, power consumption
  Increased complexity and functionnality
300mm Si wafer

## Slide 3: Main Silicon Photonics ApPlications
1310 nm – > 1Tb/s Computercom
1550 nm – > 100G  400G Metro & 10G Access
Datacenter
Routers
Switches
HPC
Rack-to-Rack
Board-to-Board
On-board
1310 nm – 100G 400G Datacom

## Slide 4: Si Photonics Building blocks at 50 Gb/s
Si or SiN
(AWG or echelle design)
1D and 2D grating couplers
Edge couplers

## Slide 5: Technology key process features
PDKs available (Cadence, Phoenix…)
Complete library with Models, Circuit simulation, Layout, Verification, Layout finishing
3D integration with electronics
Compatibility with 300 mm industrial foundry
Low parasitics 3D Photonic/Electronic Integration

## Slide 6: hETEROGENEOUS III-V INTEGRATION: Lasers, modulators, optical amplifiers
Growth of the III-V wafers
2’’, 3’’, 4’’
III-V die or wafer bonding on processed SOI + InP substrate removal
Processing of SOI wafers 200/300 mm
III-V Processing

## Slide 7: Fully integrated transmitter @ 1.3 µm for DATACOM applications
Co-integration of hybrid III-V/Si DBR laser + Si Mach-Zehnder modulator
  2.5 Vpp on each arm of the MZM (both biased @ 1.25V)
  Laser wavelength : 1303.5 nm
  Data rate : 25 Gb/s with ER=4.7 dB
25 Gb/s eye diagrams
Back-to-back
Transmission over 10 km

## Slide 8: DFB laser integrated with EAM modulator
Laser 150mA, EAM -0,6V±0,9V, SOA 90mA, PD 32GHz BW
32 Gb/s – optimal predistorsion – ER=6.7dB
Wafer bonding with single epitaxial stack

## Slide 9: Reconfigurable Silicon Photonics Switch Matrix
Next Gen ROADM: 4 directions, 12 wavelengths
384 optical switches  more than 1000 integrated photonic components, each individually electronically controlled
Flip chip assembly : 2091 microbumps

## Slide 10: What’s next : upgrade of the technology platform
Non linear optics: Broadband sources, switching, frequency conversion, …
Germanium-based lasers: laser effect demonstrated in GeSn microdisks
Photonic layer stacking

## Slide 11: What’s next : new applications
Integrated Lidar
Quantum technologies, optical computing
 On going work to develop ultra low loss optical waveguides, integrated single photon detectors, …
Chemical Sensing in the visible and Mid IR range
 next talk

## Slide 12: Conclusion / Take away
Complete platform available: design, fab, test, packaging
Key features: III-V/Si, 3D integration, new functionnalities
Silicon Photonics for high bandwidth communications
not only
… but also for many application fields